# Rockpanel Colours

A Rockpanel surface treated with triple layer water-based acrylic coating, available in a range of 24 standard colours with any RAL or NCS colour available to order (subject to 100m2 minimum quantity).

The surface has excellent UV resistance when tested in accordance with ISO 4893-1&2 and judged in accordance with ISO 105-A02 and ISO 105-A03.

Board dimensions: 3050 x 1200mm (2500 x 1200mm available in some colours)

Board thickness: 6 & 8 mm

Available in a choice of durable for general applications or Xtreme for applications where greater mechanical strength is required.

Each has the option of Protect Plus finish, which improves UV protection and provides anti-graffiti and self-cleaning finish.  The Protect Plus finish requires a minimum order quantity of 100m2 and a six week lead time.  All standard Rockpanel products have a maximum lead time of 2 weeks.

Rockpanel Colours has been awarded with several ETA certificates.

Please consult Rockpanel BV for advice on use of other Rockpanel Colours cladding products in non-ventilated constructions.

(Please delete clauses in red to suit specification)

950 FASCIAS/BARGES/SOFFITS: PRE-FINISHED STONEWOOL BOARD:

Product reference:

Rockpanel Colours Durable board

Rockpanel Colours Xtreme board

Material: Inert Rockwool panels with pre-finished decorative coating

Manufacturer: Rockwool Lapinus Productie BV, Industrieweg 15

6045 JG Roermond, The Netherlands

Sales Representative: Rockwool Rockpanel BV, Wern Tarw, Pencoed, Bridgend CF35 6NY.

Tel: 01656 863210.  Fax: 01656 863611.

E-Mail: info@rockpanel.co.uk.  Web: www.rockpanel.co.uk.

Thickness: 6mm or 8mm

Finish: Standard finish / Protect Plus Finish

Colours:

Pure White RAL 9010 /Oyster White RAL 1013/

Cream White RAL 9001 / Light Ivory RAL 1015 /

Purple Red RAL 3004 /Fir Green RAL 6009 /

Light Grey RAL 7035 / Signal Grey RAL 7004 /

Blue Grey RAL 7031 / Anthracite Grey RAL 7016 /                                                      Black Grey RAL 7021 / Jet Black RAL 9005 /

Steel Blue RAL 5011 /Terra Brown RAL 8028 / Silver Grey RAL 7001 /

Dusty Grey RAL 7037 / Stone Grey RAL 7030 / Umbra Grey RAL 7022 /

Oxide Red RAL 3009 / Black Red RAL 3007.

# Fixings:

# Rockpanel Torx screw:

Stainless steel torx head A1S1 316 grade 4.5x35mm screws, according ETA approval with colour matched heads.

Rockpanel ring shank nail:

Ring shank A1S1 316 grade stainless steel 2.7/2.9 x32 mm (flat head) nails, according ETA approval with colour matched heads.

Number and location:

6mm boards

Torx head screws fixed at maximum spans of 400mm and 300mm vertical centres.

Nails to be fixed at maximum spans of 400mm and 300mm vertical centres.

8mm boards

Torx head screws fixed at maximum spans of 600mm and 600mm vertical centres.

Nails to be fixed at maximum spans of 600mm and 400mm vertical centres.

Please consult Rockpanel BV for wind loading calculations Fixings to be positioned minimum 15mm from the vertical edge of the board and minimum 50mm from the horizontal edge of the board.

Joints

Type/treatment:

Vertical joint treatment

Flexible joint Gasket EPDM weather and UV resistant at vertical board joints

(for example; ref 090/60P of Plastestrip)

Colour: Black

Flexible joint Gasket EPDM weather and UV resistant at intermediate supports

(for example; ref 090/36P of Plastestrip)

Colour: Black

Flexible joint Gasket EPDM weather and UV resistant at vertical corner joints

(for example; ref 090/750P of Plastestrip)

Colour: Black

Note: Gaskets are fixed to increase longevity of timber battens and must be used.

### External Corner Treatment

6mm boards

Rockpanel profile D:  External corner profile (aluminium) for 6 mm board.

Rockpanel Profile E: External caped corner profile (aluminium) for 6 mm board.

8mm boards

Rockpanel profile D: External corner profile (aluminium) for 8 mm board.

Rockpanel Profile E: External caped corner profile (aluminium) for 8 mm board.

Optional:

Soffit strip ventilator for 10,000 MM² /M Air Flow for example Ref:055/10K

Colour: Colour matched to board / Black / White

Soffit strip ventilator for 25,000 MM² /M Air Flow    for example Ref:085/25L

Colour: Colour matched to board / Black / White.

Manufacturer: Plastestrip (Profiles) Ltd, 1 Enterprise Park, St Austell, Cornwall, PL25 4EJ.

Tel: 01726 74771. Fax: 01726 69238.

E-Mail: sales@plastestrip.com Web: www.plastestrip.com

Other requirements:

No gaskets required on sofft boards, providing fascia board extends 7.5mm beyond the soffit board.

Construction: Rockpanel Colours can be used in ventilated and non-ventilated constructions. For use in non-ventilated constructions, please contact Rockwool BV / Rockpanel group for advice.

Board joints:	Fascias & soffits – Maintain a 5mm gap on all vertical joints.

Maintain a gap of 5mm between the junction of the soffit board and the fascia board.

Junction of Soffit and Wall: Maintain a 5mm gap between end of soffit board and external wall face.

Support:

6mm thick Rockpanel boards

50mm x 38mm softwood timber at maximum 400mm centres with 74 x 38mm timber at vertical board joints.  All timber to be treated to Clause G20 270

8mm thick Rockpanel boards

50mm x 38mm softwood timber at maximum 600mm centres with 75 x 38mm timber at vertical board joints.  All timber to be treated to Clause G20 270

270 Ungraded Softwood for Fascia, Soffit and Barge supports.

- Quality of timber: free from decay, insect attack (except pinhole borers) and with no knots wider than half the width of the section.

- Surface finish: PSE

- Treatment: C2