Rockpanel Natural

The surface gives a natural ageing effect du to UV light, the appearance of the ageing pattern can not predict as this is the result of the actual environment and detailing, even at micro level.

Board dimensions: 3050 x 1200mm

Board thickness: 8 & 10mm

Available in a choice of durable – for general applications or Xtreme – for applications where greater mechanical strength is required and suitable for ground level installations.

Rockpanel Natural has been awarded with an ETA certificate.

Rockpanel Natural is recommended for ventilated constructions as this result’s in the most desired ageing patterns. For more information on natural aging, please contact Rockpanel BV for advice.

(Please delete Clauses in red to suit specification)

155 SHEET CLADDING………….

Product reference:

Rockpanel Natural Durable board

Rockpanel Natural Xtreme board

Material: Inert Rockwool panels without pre-finished decorative coating

Manufacturer: Rockwool Lapinus Productie BV, Industrieweg 15

6045 JG Roermond, The Netherlands

Sales Representative: Rockwool Rockpanel BV, Wern Tarw, Pencoed, Bridgend CF35 6NY.

Tel: 01656 863210.  Fax: 01656 863611.

E-Mail: info@rockpanel.co.uk.  Web: www.rockpanel.co.uk.

Thickness: 8mm or 10mm

Finish: Without any finish

Colours: Natural which discolour (mostly darkens considerable) after several months depending on the environment

# Fixings:

# Rockpanel Torx screw:

Stainless steel torx head A1S1 316 grade 4.5x35mm screws, according ETA approval with either a matt black or stainless steel finish.

Rockpanel ring shank nail:

Ring shank A1S1 316 grade stainless steel 2.7/2.9 x32 mm (flat head) nails, according ETA approval with either a matt black or stainless steel finish.

Number and location:

8mm boards

Torx head screws fixed at maximum spans of 400mm and 300 mm vertical centres.

Nails to be fixed at maximum spans of 400 mm and 300 mm

vertical centres.

10mm boards

Torx head screws fixed at maximum spans of 600mm and 600mm vertical centres.

Nails to be fixed at maximum spans of 600mm and 400mm vertical centres.

Please consult Rockpanel BV for wind loading calculations Fixings to be positioned minimum 15mm from the vertical edge of the board and minimum 50mm from the horizontal edge of the board.

Joints

Type/treatment:

Vertical joint treatment

Flexible Joint Gasket weather and UV resistance at vertical board joints

(for example ref: 090/60P of Plastestrip)

Colour: Black

Flexible Joint Gasket weather and UV resistance at intermediate supports

(for example ref: 090/36P of Plastestrip)

Colour: Black

Flexible Joint Gasket weather and UV resistance at vertical corner joints

(for example ref: 090/75P of Plastestrip)

Colour: Black

Note: Gaskets are fixed to increase longevity of timber battens and must be used.

### Horizontal Joint Treatment

8mm boards

Rockpanel profile A: Horizontal chair section (with high back) for 8 mm board (aluminium)

Rockpanel Profile B: Horizontal V-bird section (aluminium)

10mm boards

Rockpanel profile A:  Horizontal chair section (with high back) for 10 mm board (aluminium)

Rockpanel Profile B: Horizontal V-bird section (aluminium)

### External Corner Treatment

8mm boards

Rockpanel profile E: External capped corner profile for 8 mm boards (aluminium)

Rockpanel profile D: External corner profile for 8 mm boards (aluminium)

10mm boards

Rockpanel profile E: External capped corner profile for 10 mm boards (aluminium)

Rockpanel profile D: External corner profile for 10 mm boards (aluminium)

Colour: Black/ White

Distance between boards: 5mm

Air gap:  Minimum 25mm –

Consult Rockpanel for recommendations and details if designing to NHBC requirements

Support system: Timber battens as clause 230

Size: Min 75mm wide x 38mm deep at boards joints.

Min 50mm wide x 38mm deep at intermediate supports.

(Above timbers can be planed down to 70mmx28mm and 45mmx28mm respectively)

#### Fixings: number and location

Consult with Rockpanel for recommendations and details

Accessories:

Ventilated profiles:

Ref: 065/10K	bottom vent strip – from 30-65mm cavities

Ref: 090/25K	bottom vent strip – from 65-90mm cavities

Ref: 125/25K	bottom vent strip – from 90-125mm cavities

### Bottom Drips

8mm boards

Rockpanel profile J: aluminium bottom drip profile

10mm boards

Rockpanel profile J: aluminium bottom drip profile

Manufacturer: Plastestrip (Profiles) Ltd, 1 Enterprise Park, St Austell, Cornwall, PL25 4EJ.

Tel: 01726 74771. Fax: 01726 69238.

E-Mail: sales@plastestrip.com Web: www.plastestrip.com

# GENERAL REQUIREMENTS

- CONTROL SAMPLES

- General: Complete an area of the cladding and obtain

approval of appearance before proceeding.

  - Location: ……….

  - Extent of area: ……….

- TIMBER BATTENS

- General: Regularized softwood tree from decay, insect attack (except ambrosia beetle damage) and with no knots wider than half the width of the section

- Preservative treatment: As section Z12 and Wood Protection Association Preservative Treatment Commodity Specification C8.

- Type: ……………

- Moisture content at time of fixing (maximum): 19%

- TREATED TIMBER

- Exposed cut and drilled surfaces: Treat with two flood coats of a solution recommended for the purpose by main treatment solution manufacturer.

- FIXING SHEETS

- General: Secure to supports without producing distortion.

- Fasteners: Evenly spaced in straight lines, in pairs across joints and sufficient distance from edge of sheet to prevent damage.

- COVER STRIPS

- General: Form straight runs in single lengths wherever possible

- Location and method of forming joints: Submit proposals where

not detailed.