# Rockpanel Colours

A Rockpanel surface treated with triple layer water-based acrylic coating, available in a range of 20 standard colour with any RAL colour available to order (subject to minimum quantity).  The surface has excellent UV resistance when tested in accordance with ISO 4893-1&2 and judged in accordance with ISO 105-A02 and ISO 105-A03.

Board dimensions:	3050 x 1200mm (2500 x 1200mm, available in some colours)

Board thickness:  8 mm

Available in a choice of durable – for general applications or Xtreme – for applications where greater mechanical strength is required and suitable for ground level installations.

Each has the option of Protect Plus finish.  The finish improves UV protection and provides an anti graffiti finish.  The Protect Plus finish requires a minimum order quantity of 100m2 and a six week lead time.  All standard Rockpanel products have a maximum lead time of 2 weeks.

Rockpanel Colours has been awarded with several ETA certificates

Rockpanel Colours can be used in ventilated and non-ventilated constructions. For use in non-ventilated constructions, please contact Rockpanel BV for advice.

(Please delete clauses in red to suit specification)

120 Rainscreen Cladding…………

Product reference:

Rockpanel Colours Durable board

Rockpanel Colours Xtreme board

Material:	    Inert Rockwool panels with pre-finished decorative coating

Manufacturer: Rockwool Lapinus Productie BV, Industrieweg 15

6045 JG Roermond, The Netherlands

Sales Representative: Rockwool Rockpanel BV, Wern Tarw, Pencoed, Bridgend CF35 6NY.  Tel:01656 863210.  Fax: 01656 863611.

E-mail: info@rockpanel.co.uk.  Web: www.rockpanel.co.uk.

Thickness:  	    8mm for Durable Board

8mm for Xtreme Board

Finish:              Standard finish/Protect Plus Finish

Colours:           Pure White RAL 9010 / Oyster White RAL 1013 /

Cream  /White RAL 9001/ Light Ivory RAL 1015 /

Purple Red RAL 3004/Fir Green RAL 6009 /Light Grey RAL

7035 / Signal  Grey RAL 7004 / Blue Grey RAL 7031 /

Anthracite  Grey RAL 7016 / Black Grey RAL 7021 / Jet

Black  RAL 9005 / RAL 5011 Steel Blue /Terra Brown RAL

8028 /Silver Grey RAL 7001 / Dusty Grey RAL 7037

/ Stone Grey RAL 7030 / Umbra Grey RAL 7022 /

Oxide Red RAL 3009 / Black Red RAL 3007.

# Fixings	Ref:RP/fix 20 Stainless steel self tapping screws with     colour matched heads. Please note when using self tappers the maximum panel size is 1500 x 1200mm.  For larger panel sizes uses Rivets18/

Ref: Rivets/18	Stainless steel rivets with colour matched heads.  Pre-drill Rpockpanel with 9mm holes and 5.5mm for centre fixings.  A spacer tool should be used when fixing rivets.

Ref:	Riiver/spacer tool

Manufacturer:       Plastestrip (Profiles) Ltd, Trenance Mill, St Austell, Cornwall, PL25 5LZ. Tel: 01726 74771. Fax: 01726 69238.

E-mail: sales@plastestrip.com Web: www.plastestrip.com

Number and location:

8mm boards 	Rivets and self tappers to be fixed at a maximum span of 600 mm and maximum 600 mm vertical centres.

Please consult Rockpanel BV for wind loading calculations if Panels are above 9 metres

Fixings to be positioned minimum 20mm from the vertical edge of the board and minimum 50mm from the horizontal edge of the board.

Joints

Type/treatment:

If desired, blackout tape can be applied to prevent light reflection from aluminium supports.

### Horizontal joint treatment

Ref:AL/CH8	Aluminium horizontal chair section

### External Corner Treatment

8mm boards

Ref:AL/18P	External corner profile

Ref:AL/EX8	External capped profile

Colour		Colour matched to board/Black/White

Manufacturer:       Plastestrip (Profiles) Ltd, Trenance Mill, St Austell, Cornwall, PL25 5LZ. Tel: 01726 74771. Fax: 01726 69238.

E-mail: sales@plastestrip.com Web: www.plastestrip.com

Distance between boards: Minimum of 6mm

Air gap:  Minimum 25mm –

Consult Rockpanel for recommendations and details if designing to NHBC requirements

Secondary support system/framing system;

Product reference:	Plastestrip Top Hat and Z profile system

Material:		Aluminium

26mm cavity

Ref: AL/TH/26/50		Top Hat Profile

Ref:AL/Z/26/50/26	Z profile

40mm cavity

Ref: AL/TH/40/55		Top Hat Profile

Ref:AL/Z/40/55/26	Z profile

#### Fixings: number and location

Consult with Plastestrip for recommendations and details

For cavities greater than 40mm – 270mm contact Plastestrip for further details

Manufacturer:       Plastestrip (Profiles) Ltd, Trenance Mill, St Austell, Cornwall, PL25 5LZ. Tel: 01726 74771. Fax: 01726 69238.

E-mail: sales@plastestrip.com Web: www.plastestrip.com

Thermal Insulation		As clause 775

Breather membrane:	As clause 785

Accessories:

Ventilated profiles:

Ref: 025/10K	bottom vent strip – 25mm cavity

Ref: 065/10K	bottom vent strip – from 40-65mm cavities

Ref: 090/25K	bottom vent strip – from 65-90mm cavities

Ref: 125/25K	bottom vent strip – from 90-125mm cavities

### Bottom Drips

Ref: 088P		bottom drip profile

Ref: AL/BD86	aluminium bottom drip profile

Manufacturer:       Plastestrip (Profiles) Ltd, Trenance Mill, St Austell, Cornwall, PL25 5LZ. Tel: 01726 74771. Fax: 01726 69238.

E-mail: sales@plastestrip.com Web: www.plastestrip.com

# GENERAL REQUIREMENT

- GENERAL MOVEMENT

- Requirement: Rainscreen cladding must accommodate

anticipated building movements as follows……………..

- MECHANICAL FIXINGS – MECHANICAL REQUIREMENTS

- Stainless steel: To BS EN ISO 3506 grade A2 generally,

Grade A4 when used in severely corrosive environments.

- Carbon steel: To BS4190 and suitable for galvanizing or

other protective coating.

- Aluminium: To BS EN 755

- FIXINGS AND FASTENERS

- Type and use: Reviewed and approved by manufacturers.

Submit confirmatory information on request.

- Dimension: Not less than recommended by their manufacturers

- Adjustment capability: Sufficient in three dimensions to

accommodate primary support structure and rainscreen

cladding fabrication/installation tolerances.

- THERMAL INSULATION

- Material……….

- Properties: Durable, rot and vermin proof and not degradable

by moisture or water vapour.

- Fixing: Attached to the outer face or supported within the

backing wall so as not to bulge, sag, delaminate or detach

during installation or in situ during the life of the rainscreen

cladding.

- VAPOUR CONTROL LAYER

- Material………….

- Minimum vapour resistance……………..

- Manufacturer……………………………….

Product reference ……………..

- Continuity: No breaks and with the minimum of joints.

- Penetrations and abutments: Seal to vapour control layer.

If necessary, prime substrates to achieve full bond.

    - Sheet laps: not less than 150mm, seal with tape.  Prime substrates as necessary to achieve full bond

- Sheet tape: Double sided sealant with vapour resistivity not less

than the vapour control sheet.

- Size (width and thickness):……………….

- Sheet repairs and punctures: Seal with lapped patch of

vapour control membrane and continuous band of

sealant tape along edges.

- BREATHER MEMBRANE

- Material………………

- Manufacturer………….

- Product reference……………..

- Continuity: No breaks. Minimize joints.

- Penetrations and abutments: Attach to breather membrane

with tape.  Achieve full bond.

- Laps: Not less than 150mm, bond with tape.  Achieve full bond

- Tape: As recommended by breather membrane manufacturer

- Repairs: Lapped patch of breather membrane material

secured with continuous band of tape on edges.

Junctions at flashings, sills, gutters etc. Overlap and allow free

drainage to exterior.

- SEALANT APPLICATION

- Requirement: As section Z22, unless specified otherwise in this

section.

- PRELIMINARY RAINSCREEN CLADDING INSTALLATION

- Requirement: Complete an area of cladding as set out below

for inspection and approval of appearance.

- RAINSCREEN CLADDING INSTALLATION

- Tightening mechanical fasteners: To manufacturer’s

recommended torque figures.  Do not over tighten fasteners

intended to permit differential movement.

- Protective coverings: remove only where necessary to facilitate

installation and from surfaces which will be inaccessible on

completion.

- MAINTENANCE

- Maintenance manual: Incorporate details within the Building

Manual in accordance with CWCT “Standard for systemised

Building envelopes clause 7.6.1

  - Material certification and test reports to be included:

- The terms and conditions of any guarantee.

- Method statement for means of access for maintenance and for

use of any permanent equipment.

- Method statement covering the procedures for replacement of

parts that have a design life less than the design life of the

rainscreen system

- Recommendations for routine maintenance and cleaning including

suitable cleaning agents and lubrication/adjustments to working

parts.

- Record book for listing defects, maintenance and repairs.

List any supplementary contents in the clause.

The maintenance manual should schedule inspection

Requirements.  Submission requirements need to be included in

section A37