# ROCKPANEL® Colours

A ROCKPANEL surface treated with four layers water-based acrylic coating, available in a range of 20 standard colour with any RAL colour available to order (subject to minimum quantity).  The surface has excellent UV resistance when tested in accordance with TR010 and judged in accordance with EN 20105-A02. Board dimensions:	3050 x 1200mm (2500 x 1200mm, available in some colours)

Board thickness:  8 mm

Available in a choice of durable – for general applications or Xtreme – for applications where greater mechanical strength is required and suitable for ground level installations.

Each has the option of Protect Plus finish.  The finish improves UV protection and provides an anti graffiti finish.  The Protect Plus finish requires a minimum order quantity of 100m2 and a six week lead time.  All standard ROCKPANEL products have a maximum lead time of 2 weeks.

ROCKPANEL Colours has been awarded Agrément Certificate No: 04/4168

ROCKPANEL Colours can be used in ventilated and non-ventilated constructions. For use in non-ventilated constructions, please contact ROCKWOOL BV / ROCKPANEL Group for advice.

(Please delete clauses in red to suit specification)

120 Rainscreen Cladding…………

Product reference:

ROCKPANEL Colours Durable board

ROCKPANEL Colours Xtreme board

Material:	    Inert ROCKWOOL panels with pre-finished decorative coating

Manufacturer: ROCKWOOL BV / Lapinus, Industrieweg 15

6045 JG Roermond, The Netherlands

Sales Representative: ROCKWOOL BV / ROCKPANEL Group, Wern Tarw, Pencoed, Bridgend CF35 6NY.  Tel:01656 863210.  Fax: 01656 863611.

E-mail: info@rockpanel.co.uk.  Web: www.rockpanel.co.uk.

Thickness: 	8mm for Durable Board

8mm for Xtreme Board

Finish:   		Standard finish/Protect Plus Finish

Colours: 		Pure White RAL 9010/ Oyster White RAL 1013/

White RAL 9001/ Light Ivory RAL 1015/

Purple Red RAL 3004/Fir Green RAL 6009 /

Light Grey RAL 7035 / Signal  Grey RAL 7004 / Blue Grey RAL 7031 / Anthracite  Grey RAL 7016 /Black Grey RAL 7021 / Jet Black  RAL 9005 / RAL 5011 Steel Blue /Terra Brown RAL 8028 /Silver Grey RAL 7001 / Dusty Grey RAL 7037

/ Stone Grey RAL 7030 / Umbra Grey RAL 7022 /

Oxide Red RAL 3009 / Black Red RAL 3007.

# Fixings

# for Aluminium:

# Aluminium (AlMg5)Rivet with colour match head minimum Ø 14mm, length 18 mm and shank diameter 5 mm.	Pre-drill Rockpanel with 9mm holes and 5.5mm for centre fixings.  A spacer tool should be used when fixing rivets.

# Ref:RP/fix 20 Stainless steel (A4 grade) self tapping screws (thickness aluminium between 1,2 and 2,5 mm) with colour matched heads. Please note when using self tappers the maximum panel size is 1500 x 1200mm.

ROCKPANEL Tack-S system; Bonding system existing out of ROCKPANEL Tack-S for a durable adhesive connection, a double sided adhesive foam tape to secure the thickness of the glue rope and adhesion by mounting. Primer MSP transparent for the rear of the board and primer M to treat the aluminium profiles

# for steel:

# Ref:RP/fix 20 Stainless steel (A4 grade) self tapping screws with colour matched heads.

Ref:	River/spacer tool

Manufacturer/ Distributor:       Plastestrip (Profiles) Ltd, Trenance Mill, St Austell, Cornwall, PL25 5LZ. Tel: 01726 74771. Fax: 01726 69238.

E-mail: sales@plastestrip.com Web: www.plastestrip.com

Number and location:

Rivets / self tappers / ROCKPANEL Tack-S to be fixed according recommendation ROCKPANEL Group date xx-xx-xxxx.

Please consult ROCKWOOL BV /ROCKPANEL group for wind loading calculations.

Mechanical Fixings to be positioned minimum 15 mm from the vertical edge of the board and 50mm from the horizontal edge of the board.

Joints

Type/treatment:

Vertical joint treatment:

If desired, by mechanical fixing a blackout tape can be applied to prevent light reflection from aluminium supports.

### Horizontal joint treatment

ROCKPANEL profile A: Aluminium horizontal chair section (with high back) for 8 mm boards.

ROCKPANEL profile B: Aluminium horizontal V-bird section

### Open joints: minimum 6 mm, maximum 10 mm (note that a open joint system requires a cavity design which is suitable to drain penetrated rainwater and resist UV which enters through the open joints.

### External Corner Treatment

8mm boards

ROCKPANEL profile D: External corner profile (aluminium) for 8 mm boards

ROCKPANEL profile E: External capped corner profile (aluminium) for 8 mm boards

Colour		Colour matched to board/Black/White

Distance between boards: Minimum of 6mm

Air gap:  Minimum 25mm – at closed joint system

Minimum 40mm, maximum 100 mm at open joint system (note a cavity depth > 60 mm gives a main reduction of rain impact on the insulation.

Remark:

Cavity closers are necessary by an open joint system at vertical corners

Consult ROCKWOOL BV /ROCKPANEL group for recommendations and details if designing to NHBC requirements

Secondary support system/framing system;

In accordance with BBA Approval for example:

Product reference:	Plastestrip Top Hat and Z profile system

Material:		Aluminium

26mm cavity

Ref: AL/TH/26/50		Top Hat Profile

Ref:AL/Z/26/50/26	Z profile

40mm cavity

Ref: AL/TH/40/55		Top Hat Profile

Ref:AL/Z/40/55/26	Z profile

#### Fixings: number and location

Consult with Plastestrip for recommendations and details

For cavities greater than 40mm – 270mm contact Plastestrip for further details

Manufacturer:       Plastestrip (Profiles) Ltd, Trenance Mill, St Austell, Cornwall, PL25 5LZ. Tel: 01726 74771. Fax: 01726 69238.

E-mail: sales@plastestrip.com Web: www.plastestrip.com

Thermal Insulation		As clause 775

Breather membrane:	As clause 785

ROCKPANEL Accessories:

### Bottom Drips(optional)

ROCKPANEL profile J:	aluminium bottom drip profile

General Accessories:

Ventilated profiles:

Ref: 025/10K	bottom vent strip – 25mm cavity

Ref: 065/10K	bottom vent strip – from 40-65mm cavities

Ref: 090/25K	bottom vent strip – from 65-90mm cavities

Ref: 125/25K	bottom vent strip – from 90-125mm cavities

Manufacturer:       Plastestrip (Profiles) Ltd, Trenance Mill, St Austell, Cornwall, PL25 5LZ. Tel: 01726 74771. Fax: 01726 69238.

E-mail: sales@plastestrip.com Web: www.plastestrip.com

# GENERAL REQUIREMENT

- GENERAL MOVEMENT

- Requirement: Rainscreen cladding must accommodate

anticipated building movements as follows……………..

- MECHANICAL FIXINGS – MECHANICAL REQUIREMENTS

- Stainless steel: To BS EN ISO 3506 grade A2 generally,

Grade A4 when used in severely corrosive environments.

- Carbon steel: To BS4190 and suitable for galvanizing or

other protective coating.

- Aluminium: To BS EN 755

- FIXINGS AND FASTENERS

- Type and use: Reviewed and approved by manufacturers.

Submit confirmatory information on request.

- Dimension: Not less than recommended by their manufacturers

- Adjustment capability: Sufficient in three dimensions to

accommodate primary support structure and rainscreen

cladding fabrication/installation tolerances.

- THERMAL INSULATION

- Material……….

- Properties: Durable, rot and vermin proof and not degradable

by moisture or water vapour.

- Fixing: Attached to the outer face or supported within the

backing wall so as not to bulge, sag, delaminate or detach

during installation or in situ during the life of the rainscreen

cladding.

- VAPOUR CONTROL LAYER

- Material………….

- Minimum vapour resistance……………..

- Manufacturer……………………………….

Product reference ……………..

- Continuity: No breaks and with the minimum of joints.

- Penetrations and abutments: Seal to vapour control layer.

If necessary, prime substrates to achieve full bond.

    - Sheet laps: not less than 150mm, seal with tape.  Prime substrates as necessary to achieve full bond

- Sheet tape: Double sided sealant with vapour resistivity not less

than the vapour control sheet.

- Size (width and thickness):……………….

- Sheet repairs and punctures: Seal with lapped patch of

vapour control membrane and continuous band of

sealant tape along edges.

- BREATHER MEMBRANE

- Material………………

- Manufacturer………….

- Product reference……………..

- Continuity: No breaks. Minimize joints.

- Penetrations and abutments: Attach to breather membrane

with tape.  Achieve full bond.

- Laps: Not less than 150mm, bond with tape.  Achieve full bond

- Tape: As recommended by breather membrane manufacturer

- Repairs: Lapped patch of breather membrane material

secured with continuous band of tape on edges.

Junctions at flashings, sills, gutters etc. Overlap and allow free

drainage to exterior.

- SEALANT APPLICATION

- Requirement: As section Z22, unless specified otherwise in this

section.

- PRELIMINARY RAINSCREEN CLADDING INSTALLATION

- Requirement: Complete an area of cladding as set out below

for inspection and approval of appearance.

- RAINSCREEN CLADDING INSTALLATION

- Tightening mechanical fasteners: To manufacturer’s

recommended torque figures.  Do not over tighten fasteners

intended to permit differential movement.

- Protective coverings: remove only where necessary to facilitate

installation and from surfaces which will be inaccessible on

completion.

- MAINTENANCE

- Maintenance manual: Incorporate details within the Building

Manual in accordance with CWCT “Standard for systemised

Building envelopes clause 7.6.1

  - Material certification and test reports to be included:

- The terms and conditions of any guarantee.

- Method statement for means of access for maintenance and for

use of any permanent equipment.

- Method statement covering the procedures for replacement of

parts that have a design life less than the design life of the

rainscreen system

- Recommendations for routine maintenance and cleaning including

suitable cleaning agents and lubrication/adjustments to working

parts.

- Record book for listing defects, maintenance and repairs.

List any supplementary contents in the clause.

The maintenance manual should schedule inspection

Requirements.  Submission requirements need to be included in

section A37